

The Fabrication Lab

**New Materials Testing Guide**

**Aim**

The aim of this document is to provide a guideline for the testing of the cutting and etching of new materials with the Fabrication Lab Rayjet EDU 300 Laser Cutter. This document is a guideline only and does not cover all eventualities in testing new materials, therefore, extreme caution should be used when using the laser cutter with a new material.

**Method**

* Identify the material.
* Obtain the Material Safety and Data Sheet (MSDS) for the material. MSDS sheets can be obtained through google searches or from <http://www.msds.com>.
* Examine the MSDS for ‘Hazards’ and ‘Hazard Identification’ sections, particularly hazards related to heating the material. For example from the Medium Density Fiberboard (MDF) MSDS:



While the laser cutter is equipped with a HEPA air filter, ALL gas release may be hazardous, so any materials releasing toxic fumes may not be used without express exception permission from senior Fabrication Lab management.

If unsure of a material or the data contained within the MSDS, contact the manufacturer and enquire about laser cutting of the material.

The following materials are known to be hazardous:

* Polyvinylchloride (PVC) based materials.
* Materials containing melamine resins.
* Plastics containing Nylon.
* High Density Foam or other materials containing polyurethane.
* MDF or Plywood or other materials containing either urea- or phenol-formaldehyde.
* Foam-core board or other materials containing Polystyrene or Styrene.

**If you unsure of the type of plastic you are dealing with refer to *Polymer Identification[[1]](#footnote-1)* document from this link.** <http://www.chymist.com/polymers.html>

* If the material is a reflective material such as a glass or mirror surface, it is recommended to cut from the non-reflective side if available.
* If the material is found to be suitable for cutting, setup the material and focus the laser as per standard Edge Laser Cutter Induction procedure
* In CorelDraw, create a small 20mm x 20mm square set to RED Hairline.

**For low density materials or materials LESS than 2mm thick:**

1. In the Rayjet print preferences, set the RED CUTTING setting Power to 5% and Speed to 5% with a single pass.
2. Select skip in the BLACK ENGRAVING option.
3. Set ‘Move job to Laser’ in the laser print spooler.
4. Perform this cut.
5. Move laser to top left corner away from material.
6. Remove material and examine cut. Mark the Power and Speed settings in the format POWER/SPEED next to the cut. i.e. 5/5.
7. If the cut did not penetrate the material completely, perform the procedure again from Step 8 using an increment of 5% in Power
8. It is important to make successive cuts next to each other in an ordered pattern and note the power/speed for each cut.
9. Repeat the procedure increasing the power until a complete cut is made. At this point, fine tune the settings using 1-2% increments or decrements, taking note on the test material for each cut.

**For high density materials or materials more than 2mm thick:**

1. In the Rayjet print preferences, set the RED CUTTING setting Power to 5% and Speed to 5% with TWO passes.
2. Select skip in the BLACK ENGRAVING option.
3. Set ‘Move job to Laser’ in the laser print spooler.
4. Perform this cut.
5. Move laser to top left corner away from material.
6. Remove material and examine cut. Mark the Power and Speed settings in the format POWER/SPEED next to the cut. i.e. 5/5.
7. If the cut did not penetrate the material completely, perform the procedure again from Step 8 using an increment of 5% in Power
8. It is important to make successive cuts next to each other in an ordered pattern and note the power/speed for each cut.
9. Repeat the procedure increasing the power until a complete cut is made. At this point, fine-tune the settings using 1-2% increments or decrements, taking note on the test material for each cut.
* Once successful cuts have been made, examine the cut edges. If these are smooth and straight note down the cut settings for use. If the edges are melted or beveled / rounded, you may need to increase the passes, in which case, perform the procedure from the 5/5 % setting start again.
* Once settings have been found for cutting, test for engraving as follows:
1. In CorelDraw, create a small 20mm x 20mm square set to filled with BLACK.
2. In the Rayjet print preferences, set the **BLACK ENGRAVING** setting Power to 5% and Speed to 50%.
3. Select skip in the RED CUTTING option.
4. Set ‘Move job to Laser’ in the laser print spooler.
5. Perform this engrave.
6. Move laser to top left corner away from material.
7. Remove material and examine cut. Mark the Power and Speed settings in the format POWER/SPEED next to the engrave. i.e. 5/50.
8. If the cut did not penetrate the material completely, perform the procedure again from Step 8 using an increment of 5% in Power
9. It is important to make successive engraves next to each other in an ordered pattern and note the power/speed for each engrave.
10. Repeat the procedure increasing the power until a good deep engrave is performed. At this point, fine tune the settings using 1-2% increments or decrements, taking note on the test material for each cut.
11. If 100% power is reached and with 50% speed and the engrave is not sufficient, set power to 90% and reduce the speed until desire engraving depth is reached.
* As with normal operation, the laser cutter must always be monitored during operation in case of smoke, fire or flare up.

**References:**

Harvard Fab Lab, n.d. Laser Training Checklist, Retrieved 27 May 2015 from <http://isites.harvard.edu/fs/docs/icb.topic1198394.files/training_checklist_LASER.pdf>

David A. Katz, Identification of Polymers ©1998 Retrived 31 Aug 2015 <http://www.chymist.com/polymers.html>

**Creative Commons license**

© State of Queensland (State Library of Queensland) 2020

This policy is licensed under a Creative Commons Attribution 3.0 Australia licence. You are free to copy, communicate and adapt this work, so long as you attribute the State Library of Queensland.

  

 For more information see <http://creativecommons.org/licenses/by/3.0/au>

1. [↑](#footnote-ref-1)